## A successful Czech (hence, EU) test of fire resistance of a plastered strawbale wall
As Jan Růžička announced on the ESBG in Bouzov already, a specimen of a loadbearing strawbale wall, a 3 m square 0.58 m thick has been subjected to a standard fire test in June 2011. The inner (heated) side has been earth-plastered (5 cm), the outer side had a lime plaster (3 cm). Bales had 77 kg/m3 originally and 93 kg/m3 when fixed in the specimen. During the test, the load on the specimen had been 12 kN/m (so, like 360 kg on the whole specimen). The wall had endured for 144 min, test had been stopped due to the vertical deformation exceeding the allowed limit – this happend shortly after a large part of the earth plaster fell down.
Another pair of specimens has been tested as well, one of them using strawbales as insulation (41 cm thick) in a wooden construction, earth plastered. This test had to be finished after 69 min due to a failure of the other specimen; the strawbale-filled one remained almost intact – so it had been declared to comply with requirements for at least 60 min.
The outcome has been achieved with the financial support of the Program Efekt of the Ministry of Industry and Trade of the Czech Republic within the Project 1221420507: Selected Properties of Natural Based and Other Materials, Structural Components and Buildings. Project leader: Jan Růžička, jan.ruzicka at fsv.cvut.cz, Faculty of Civil Engineering, CTU in Prague, Department of Building Structures. Project partners for the preparation of the first specimen: ABatelier (abrotanek at pasivnidomy.cz) and Hliněné omítky Picas (navratil at rigi.cz).
Czech info on the project is http://kps.fsv.cvut.cz/index.php?lmut=cz&part=vyzkum&sub=30 , the Czech-written official protocol from the first test can be downloaded there by http://kps.fsv.cvut.cz/file_download.php?fid=2346 as a file protokol_pr-11-2.097.pdf (the second test protocol has the final numbers larger by 1).
An excellent slideshow with images, captions and graphs, by Jan Ruzicka and Marek Pokorny, is available either in a 95 MB zip file of all Bouzov lectures http://www.slamenestavitelstvi.cz/esbg/download/ESBC-Slides.zip or separately as a 3 MB file http://amper.ped.muni.cz/jenik/straw/tests/FireTest_JanRuzicka.pdf.

The present short info with some uncommented images is available in the same directory http://amper.ped.muni.cz/jenik/straw/tests/ as FireTestStrawCZ.pdf. Info prepared Nov 11 by Jenik Hollan using a Czech leaflet by Aleš Brotánek.